Supplemental Table 1. X-ray diffraction data from Carlsbad Cavern cave pearls. Mole percent Mg calculated using Lumsden (1979) after correcting the (104) peak using a quartz standard.

| Location | Sample Name | Description | Aragonite present (d = 3.40) | Calcite (104) d-spacing, corrected | mole % Mg |
| --- | --- | --- | --- | --- | --- |
| Rookery | CC090806-01X-1 | white core | yes | 3.0212 | 4.9 |
| Rookery | CC090806-01AX-1 | middle cortex | no | 3.0153 | 6.9 |
| Rookery | CC090806-01AX-2 | outer dark edge | yes | 3.0098 | 8.7 |
| Lower Cave | CC080724-01AX-1 | outer dark grey | yes, trace | 3.0196 | 5.5 |
| Lower Cave | CC080724-01AX-2 | inner light grey | yes, trace | 3.0220 | 4.7 |
| Secondary Stream Passage | CC090808-2X-1 | white core | no | 3.0331 | 1.0 |
| Secondary Stream Passage | CC090808-2X-2 | tan cortex | no | 3.0287 | 2.4 |